**Shanghai Sheeny Metal Mateirals Co.,Ltd.**

|  |
| --- |
| **Tel : +86-400-663-2276 Web: www.eternal-element.cn**  **E-Mail :** [**sales@eternal-element.com**](mailto:sales@eternal-element.com) **Address :** **560 Suide Road, Putuo District, Shanghai** |

|  |
| --- |
| ★**Products** |

图片包含 文本

描述已自动生成COA Encoding :

Product Name : Neodymium Oxide

CAS.No ：1313-97-9

Molecular Formula ：Nd2O3

徽标

低可信度描述已自动生成Lot Number :

Purity : 99.999%

Particle Size（D50） : 3-6 μm

|  |  |  |  |
| --- | --- | --- | --- |
| Element | Content [%] | Element | Content [ppm] |
| La2O3 | ≤1 | Fe2O3 | ≤2 |
| CeO2 | ≤1 | SiO2 | ≤20 |
| Pr6O11 | ≤1 | CaO | ≤10 |
| Nd2O3 | 99.999% | Al2O3 | ≤2 |
| Sm2O3 | ≤1 | MgO | ≤5 |
| Eu2O3 | ≤1 | PbO | ≤2 |
| Gd2O3 | ≤0.5 | NaO | ≤5 |
| Tb4O7 | ≤0.5 | NiO | ≤2 |
| Dy2O3 | ≤0.5 | P | ≤5 |
| Ho2O3 | ≤0.5 | S | ≤20 |
| Er2O3 | ≤0.5 | Cl | ≤50 |
| Tm2O3 | ≤0.5 | REO | ＞99.5% |
| Yb2O3 | ≤0.5 | LOI | ＜1% |
| Lu2O3 | ≤0.5 |  |  |
| Y2O3 | ≤1 |  |  |

**★元素杂质含量**

This analysis sheet is only used for the batch number of the contract corresponding to the customer who purchased our company's products, and does not represent the quality of all our products under the same specifications. Specific indicator requirements can be confirmed with our sales personnel!

|  |
| --- |
| “Thank you for your long-term care and support to our company” |
| ⓒ Copyright 2023 Shanghai Sheeny Metal Mateirals Co.,Ltd. |