**Shanghai Sheeny Metal Mateirals Co.,Ltd.**

|  |
| --- |
| **Tel : +86-400-663-2276 Web: www.eternal-element.cn** **E-Mail :** **sales@eternal-element.com** **Address :** **560 Suide Road, Putuo District, Shanghai** |

|  |
| --- |
| ★**Products** |

COA Encoding :

Product Name : Praseodymium Oxide

CAS.No ：12037-29-5

Molecular Formula ：Pr6O11

Lot Number :

Purity : 99.9%

Particle Size（D50） :10-20μm

|  |  |  |  |
| --- | --- | --- | --- |
| Element | Content [%] | Element | Content [%] |
| Pr6O11 | 99.9% | Fe2O3 | ＜0.005 |
| La2O3 | Total ≤0.1% | SiO2 | ＜0.01 |
| CeO2 | CaO | ＜0.03 |
| Nd2O3 | Al2O3 | ＜0.01 |
| Sm2O3 | MgO |  No Detect  |
| Eu2O3 | PbO |  No Detect  |
| Gd2O3 | NaO |  No Detect  |
| Tb4O7 | NiO |  No Detect  |
| Dy2O3 | P |  No Detect  |
| Ho2O3 | S |  No Detect  |
| Er2O3 | Cl | ＜0.03 |
| Tm2O3 | REO | ＞99% |
| Yb2O3 | LOI | ＜1% |
| Lu2O3 |  |  |
| Y2O3 |  |  |

**★元素杂质含量**

This analysis sheet is only used for the batch number of the contract corresponding to the customer who purchased our company's products, and does not represent the quality of all our products under the same specifications. Specific indicator requirements can be confirmed with our sales personnel!

|  |
| --- |
| “Thank you for your long-term care and support to our company” |
| ⓒ Copyright 2023 Shanghai Sheeny Metal Mateirals Co.,Ltd. |